## Slide 1: The electronic structure of GdN from x-ray spectroscopy
Andrew Preston
andrew@preston.co.nz
Department of Physics
Boston University

## Slide 2: NML at BU
Kevin Smith
Louis Piper
Sang Wan Cho
Alex DeMasi

## Slide 3: Co-authors
Ben Ruck, Joe Trodahl
  Victoria University of Wellington, New Zealand
Walter Lambrecht
  Case Western Reserve
James Downes
  Macquari University, Australia
Louis Piper, Kevin Smith
  Boston University

## Slide 4: Overview
High quality thin films
Temperature dependant
X-ray at the N K- and Gd M-edges
  Absorption
  Emission
  Resonant emission

## Slide 5: GdN
Half-filled 4f shell
Phys. Rev. B 73, 235335 (2006)
  Semiconducting
  Ferromagnetic 70 K
Phys. Rev. B 76, 085211 (2007)
  Optical redshift
J. Appl. Phys. 106, 063910 (2009)
  Epitaxial GdN
  n ~ 4 x 1020 cm-3
  Negative magnetoresistance
  YSZ capping layer

## Slide 6: X-ray absorption (XAS)
Ef
Empty
Filled

## Slide 7: X-ray absorption (XAS)
Ef
Empty
Filled

## Slide 8: X-ray emission (XES)
Ef
Empty
Filled

## Slide 9: Band structure
Notes: Gd 4f bands at 5 eV
VB is made up of N p bands
CB is made up of Gd 5d and 6s bands
Optical gap at X

## Slide 10: Band structure
Notes: N p-projected character. Very little hybridization with 4f bands.
At CBM there is no N p-character between G-X, but along X-K and X-W.

## Slide 11: N K-edge XXS
Notes: Occupied and unoccupied states.
XES is from N p-like valence band states. Shoulder is from states between G-X, G-K and at L.
XAS is the N p-like character of the unoccupied Gd 5d and 6s states.
Two main peaks are the Gd 5d crystalfield split t2g (N pi) and eg (N sigma) anti-bonding states.

## Slide 12: ReN N K-edge XAS
Notes: Across series peak B is stationary, peak C shifts to higher energy. Attributed to differences in N pi/sigma bond with Re 5d crystal field split states.

## Slide 13: N K-edge XXS
Notes: Excellent agreement between experiment and theory. Aligned by main XES peak (no shift between XAS and XES).
B and C explained by Gd 5d states.
Where does double peak structure and peak A come from?

## Slide 14: Spin-resolved PDOS
Notes: All due to spin-split nature of band structure

## Slide 15: M-edge XAS and XES
Notes: XAS: fairly typical atomic multiplet spectrum. Gd 3+ calculation.
XES: low resolution, note 5p peak.
4f final states of 4f8 and 4f6 for XAS and XES are same as XPS/BIS final states.
Estimate the 4f splitting as published for XPS/BIS – get 12.5 eV, roughly the same result

## Slide 16: Thanks
Appl. Phys. Lett. submitted